## Slide 1
University of St Andrews
Andy Mackenzie
University of St Andrews, Scotland
Max Planck Institute for Chemical Physics of Solids, Dresden
Probing low temperature phase formation in Sr3Ru2O7
CIFAR Summer School May 2013

## Slide 2
Sources
S.A. Grigera et al., Science 306, 1154 (2004).
S.A. Grigera et al., Phys. Rev. B 67, 214427 (2003).
R.S. Perry et al., Phys. Rev. Lett. 92, 166602 (2004).
R.A. Borzi et al., Science 315, 214 (2007).
http://research-repository.st-andrews.ac.uk/handle/10023/837
A.W. Rost et al., Science 325, 1360 (2009).
A.W. Rost et al., Proc. Nat. Acad. Sci. 108, 16549 (2011).
D. Slobinsky et al., Rev. Sci. Inst. 83, 125104 (2012).
A.W. Rost, PhD thesis, University of St Andrews

## Slide 3
Contents
Introduction: discovery using resistivity of new phenomena in Sr3Ru2O7.
3. A.c. susceptibility as a probe of first order phase boundaries.
4. Using the magnetocaloric effect to measure field-dependent entropy.
2. Measuring magnetisation using Faraday force magnetometry.
5. Probing second order phase transitions with the specific heat.
6. Summary.

## Slide 4
Magnetoresistance of ultra-pure single crystal Sr3Ru2O7
T = 100 mK
l = 3000 Å
R.S. Perry et al., Phys. Rev. Lett. 92, 166602 (2004).

## Slide 5
Does this strange behaviour of the resistivity signal the formation of one of more new phases?
T = 100 mK
l = 3000 Å

## Slide 6
Low temperature magnetisation of Sr3Ru2O7
T ~ 70 mK
ΔM ~ 10-4 (μB/Ru)/√Hz
2 cm
Lightweight plastic construction Faraday force magnetometer: Sample of magnetic moment m experiences a force if placed in a field gradient:
Detection of movement of one plate of a spring-loaded capacitor.
D. Slobinsky et al., Rev. Sci. Inst. 83, 125104 (2012).

## Slide 7
Low temperature magnetisation of Sr3Ru2O7
T ~ 70 mK
ΔM ~ 10-4 (μB/Ru)/√Hz
1 cm
Three distinct ‘metamagnetic’ features, i.e. superlinear rises in magnetisation as a function of applied magnetic field.
Are any of these phase boundaries?

## Slide 8
as an amplitude proportional to pick-up coil area A, number of turns n and measurement frequency and a phase (for ideal mutual inductance 90 degrees)
Two coils, opposite sense of connection implies zero signal; classic null method.
Probing first-order phase transitions using mutual inductance
Voltage induced in red pick-up coil due to time-varying field produced by blue drive coil.

## Slide 9
Now insert a sample in one coil: you get a complex signal back depending on the properties of the sample.
’’
Real part of a.c. magnetic susceptibility due to ideal response of the sample: where M is the sample magnetisation (neglecting subtle dynamical effects).
Imaginary part which will only appear due to dissipation on crossing a 1st order phase boundary.
N.B. Dissipation in an a.c. measurement has the same roots as hysteresis in a d.c. one.
Possibility of a dissipative response

## Slide 10
Twin ‘pickup’ coils each > 1000 turns of insulated Cu wire 10 μm in diameter; one contains the crystal.
‘Modulation’ coil of superconducting wire providing a.c. field h0 up to 100 G r.m.s. at 20 Hz
Cryomagnetic system: 18 T superconducting magnet, base T 25 mK,
noise floor ~10pV/√Hz @ baseT, maximum B
Coil craft: Alix McCollam, Toronto
State-of-the-art a.c. susceptibility

## Slide 11
Problem – signal amplification system contains unknown capacitance and inductance, so the absolute phase of the signal is not easily known:
’’
’’
X and Y channels of lock-in will both contain components of both and is ubiquitous but is rare, try to find by maximising and check very carefully if this leaves you any signal at in the channel. If it does, there is some dissipation.
Key challenge in real life: establishing the absolute phase

## Slide 12
Susceptibility results from ultrapure Sr3Ru2O7
S.A. Grigera et al., Science 306, 1154 (2004).
R.S. Perry et al., Phys. Rev. Lett. 92, 166602 (2004).
R.A. Borzi et al., Science 315, 214 (2007).
T = 1 K
T = 100 mK
T = 500 mK
Examination of temperature and field dependence validates phase analysis.

## Slide 13
Direct comparison between susceptibility and resistivity
Sharp changes in resistivity correspond to first order phase transitions
Susceptibility signal corresponding to the broad low-field metamagnetic feature
T = 100 mK
R.S. Perry et al., Phys. Rev. Lett. 92, 166602 (2004).

## Slide 14
Susceptibility results from ultrapure Sr3Ru2O7
S.A. Grigera et al., Science 306, 1154 (2004).
R.S. Perry et al., Phys. Rev. Lett. 92, 166602 (2004).
R.A. Borzi et al., Science 315, 214 (2007).
T = 1 K
T = 100 mK
T = 500 mK
Examination of temperature dependence validates phase analysis.

## Slide 15
The low temperature phase diagram of Sr3Ru2O7 mark I
S.A. Grigera et al., Science 306, 1154 (2004).
7.9
8.1
8.3
7.7
oH (T)
0.4
0.8
1.2
0
T(K)
Outward curvature was a surprise – if these really are first order transitions, the magnetic Clausius-Clapeyron equation
implies that the entropy between the two phase boundaries is higher than that outside it. Unusual (though not unprecedented) for a phase.

## Slide 16
‘Any method involving the notion of entropy, the very existence of which depends on the second law of thermodynamics, will doubtless seem to many far-fetched, and may repel beginners as obscure and difficult of comprehension.’
W. Gibbs (1873)
Independent measurement of entropy change as a function of magnetic field

## Slide 17
Copper Ring
CuBe Springs
Kevlar Strings (35 @ 17μm)
Silver Platform
with sample
on other side
Thermometer
(Resistor)
2 cm
The magnetocaloric effect
Under adiabatic conditions
This is just the principle that governs the cooling of cryostats by adiabatic demagnetisation; here we use it to determine the field change of entropy.
http://research-repository.st-andrews.ac.uk/handle/10023/837
A.W. Rost, PhD thesis, University of St Andrews
Notes: dS = dQ/T = C/Tdt and negative sign corresponds to heat flowing from the sample.

## Slide 18
Adiabatic conditions; 1st order transition at to
Non-adiabatic conditions (can be controlled by coupling sample platform to bath with wires of known thermal conductivity).
Two different modes of operation

## Slide 19
H [T]
T [mk]
Metamagnetic
crossover seen in susceptibility
Sharper features associated with first order transitions
Sample raw Magnetocaloric Effect data from Sr3Ru2O7
‘Signs’ of changes confirm that entropy is higher between the two first order transitions than outside them.

## Slide 20
Entropy jump at first order phase boundary from direct analysis of MCE data
Entropy jump determined independently from magnetisation data and Clausius Clapeyron relation
Quantitative thermodynamic consistency

## Slide 21
Two phase boundaries definitely established
S.A. Grigera et al., Science 306, 1154 (2004).
Green lines definitely first-order transitions; what about the ‘roof’?
For this, the experiment of choice is the heat capacity.
A.W. Rost et al., Science 325, 1360 (2009).
7.9
8.1
8.3
7.7
oH (T)
0.4
0.8
1.2
0
T(K)

## Slide 22
Copper Ring
CuBe Springs
Kevlar Strings (35 @ 17μm)
Silver Platform
with sample
on other side
Thermometer
(Resistor)
2 cm
Our specific heat rig – just the magnetocaloric rig plus a heater.
Heater is a 120 Ω thin film strain gauge attached directly to the sample with silver epoxy
Notes: dS = dQ/T = C/Tdt and negative sign corresponds to heat flowing from the sample.

## Slide 23
Time constant of decay in stage 3 is proportional to C/k where C is the sample heat capacity and k is the thermal conductance of the link to the heat bath.
The relaxation time method for measuring specific heat
This ‘relaxation’ measurement principle is used in the Quantum Design PPMS.
No heat
Heat at constant rate
No heat

## Slide 24
Specific heat on cooling into the phase
Clear signal of a second order phase transition but against the unusual background of a logarithmically diverging C/T.
μoH = 7.9 T
7.9
8.1
8.3
7.7
oH (T)
0.4
0.8
1.2
0
T(K)

## Slide 25
11 T
6 T
7.9 T
7.9
8.1
8.3
7.7
oH (T)
0.4
0.8
1.2
0
T(K)
Rising C/T is a property of the phase and not its surroundings
Although the phase is metallic it seems to be associated with degrees of freedom additional to those of a standard Fermi liquid.
A.W. Rost et al., Proc. Nat. Acad. Sci. 108, 16549 (2011).

## Slide 26
Third boundary established – this is a novel quantum phase
S.A. Grigera et al., Science 306, 1154 (2004).
Green lines are first-order transitions, dark blue are second order.
A.W. Rost et al., Science 325, 1360 (2009).
7.9
8.1
8.3
7.7
oH (T)
0.4
0.8
1.2
0
T(K)
A.W. Rost et al., Proc. Nat. Acad. Sci. 108, 16549 (2011).

## Slide 27
The bigger picture
Phase appears to have a nematic order parameter and to form against a background of quantum criticality.
A.P. Mackenzie et al., Physica C 481, 207 (2012)

## Slide 28
University of St Andrews
Summary
CIFAR Summer School May 2013
The magnetocaloric effect, a.c. susceptibility and the specific heat are all effective probes of the formation of novel quantum phases.
Moral
Microscopics are all well and good, but never forget the power of thermodynamics in investigating many-body quantum systems.